## Slide 1
Numerical Modelling of Steel Fibre Reinforced Concrete Tunnel lining Segment Subjected to Flexure
Manas Bhadury, Dr. Keerthana Kirupakaran and Dr. Ravindra Gettu
Building Technology, Construction Materials and Management (BTCM) group
Department of Civil Engineering
Indian Institute of Technology Madras, Chennai, India

## Slide 2: Background
Transient stage: stacking, handling, transportation
Bending stresses
Construction stage: TBM jack thrust forces
Splitting and spalling stresses
Service stage: Soil, rock, water pressure
Increase in bending moment and axial forces
Zhou et al. (2024) Stephen et al. (2019)
Background
Methodology
Numerical modelling
Conclusions

## Slide 3
Numerical modelling: Alternative to the large-scale experiment.
Aim: To predict the flexural capacity of tunnel segment using a robust numerical framework and validate the model with full scale experimental results.
Addition of fibres to have better crack control
Experimental investigation: Performing large scale
experiment is difficult.
Difficulties:
Complex material model
Nonlinear analysis
Fibres
Background
Background
Methodology
Numerical modelling
Conclusions

## Slide 4: Modelling- Methodology
Key elements:
How to get the tensile constitutive law?
How to decide on the element size of the tunnel segment model?
Which type of nonlinear analysis is better to give stable post peak results?
How do we incorporate the loading rate effect in our finite element model?
Constitutive law
Inverse analysis
2D Tunnel model
Nonlinear analysis
Cracking pattern, load-deflection curves
Background
Methodology
Numerical modelling
Conclusions

## Slide 5: Modelling- Material parameters
Constitutive law:
Background
Methodology
Numerical modelling
Conclusions
Parameters | Optimized values
w1, 𝜎1 | 0, 3.048
w2, 𝜎2 | 0.047, 1.260
w3, 𝜎3 | 0.892, 1.733
w4, 𝜎4 | 2.062, 2.079
w5, 𝜎5 | 15, 0
Inverse analysis:
In compression
In tension
Performing uniaxial tension test is difficult
Experiment
Inverse analysis
Olesen et al. (2001), Stephen et al. (2019), Raphael et al. (2003)
Closed form solution

## Slide 6: Modelling – Inverse analysis
Assumptions:
48 number of interface elements.
3-point newton-cotes integration scheme for interface elements
Normal and shear stiffness of the interface elements = 108 N/mm
Schellekens et al. (1993)
Background
Methodology
Numerical modelling
Conclusions
Parameters | Optimized values
w1, 𝜎1 | 0, 3.048
w2, 𝜎2 | 0.047, 1.260
w3, 𝜎3 | 0.892, 1.733
w4, 𝜎4 | 2.062, 2.079
w5, 𝜎5 | 15, 0
To avoid oscillatory traction profile

## Slide 7: Modelling – Tunnel segment
crack band-width=element size
Tunnel segment modelling
Crack location not known apriori
Smeared crack model
Total strain crack model
Fixed
Rotating
Crack direction will depend on the direction of principal strain
Bazant et al. (1983), DiANA FEA manual
Background
Methodology
Numerical modelling
Conclusions

## Slide 8: Tunnel segment – experimental details
Background
Methodology
Numerical modelling
Conclusions
L1,L2,L3 – Mid-span deflection
L4 – Quarter-span deflection
L7, L10 – Support deflection
L5, L6, L8, L9 – Specimen sliding

## Slide 9: Tunnel model – flow chart
Background
Methodology
Numerical modelling
Conclusions
Model geometry
Material properties
Mesh
Loading and boundary condition
Nonlinear analysis
Results
Through mesh sensitivity analysis
Load-controlled and displacement- controlled analyses are compared
Load-deflection curves and contour plots

## Slide 10: Modelling – Tunnel segment
Mesh sensitivity analysis
Mesh1:220 elements
Mesh2: 1140 elements
Mesh3: 2520 elements
8 noded quadratic plane stress elements
In this study, 60 mm (Mesh1) mesh size is chosen which is equal to the length of steel fibre
Background
Methodology
Numerical modelling
Conclusions

## Slide 11: Loading pattern
Loading pattern
Loading was imposed through a plywood plate in the experiment (Load controlled)
Loading pattern in the numerical model
Load controlled
Displacement controlled
Background
Methodology
Numerical modelling
Conclusions
Load controlled
Displacement controlled

## Slide 12
Nonlinear analysis
Displacement controlled
Load controlled with arc length
Equal displacement is prescribed over the three nodes
Modelling - Nonlinear analysis
Background
Methodology
Numerical modelling
Conclusions

## Slide 13: Modelling - Nonlinear analysis
Nonlinear analysis
Displacement controlled
Load controlled with arc length method
Analysis 1 load-controlled
Analysis 2 with arc length
Vertical displacements of the nodes are controlled by using adaptive load factor
Background
Methodology
Numerical modelling
Conclusions

## Slide 14
Load controlled
(analysis 1)
Arc length (analysis 2)
Regular newton Raphson is used as iterative method.
Modelling - Nonlinear analysis
Background
Methodology
Numerical modelling
Conclusions

## Slide 15: Modelling - Results
This nodal deflection corresponds to the reading of L1, L2, L3
Background
Methodology
Numerical modelling
Conclusions

## Slide 16: Load controlled vs displacement controlled
Load vs Displacement controlled analysis
Displacement control
Load control
Strain is more localized in the neighbouring elements than the middle elements.
Strain is more localized in the middle elements
Middle crack in the experiment
Background
Methodology
Numerical modelling
Conclusions
Load controlled analysis along with arc length method is adopted

## Slide 17
A
C
B
Principal strain contour at C
Principal stress contour at C
Background
Methodology
Numerical modelling
Conclusions
Modelling – Stress, Strain contours
Principal strain contour at A
Principal stress contour at A
Principal strain contour at B
Principal stress contour at B

## Slide 18: Modelling – Rate effect
Notched beam test with standard CMOD rate
Tensile constitutive law from inverse analysis
Modify the constitutive law for different CMOD rates
Input for tunnel model
= tensile strength of concrete at the CTOD rate
= tensile strength of FRC at the standard loading rate
𝜎𝑖,𝑥 is the different bridging stresses at the CTOD rate
𝑓𝑡,𝑐𝑜𝑛𝑐,𝑠𝑡𝑑 is the tensile strength of plain concrete at the standard CMOD rate
Stephen et al.(2019)
Purpose:
How can we incorporate effect of loading rate in the numerical model?
Background
Methodology
Numerical modelling
Conclusions

## Slide 19
Modification of constitutive law
FEA with slower loading rate has a very good match with the experiment.
Modelling – Rate effect
Background
Methodology
Numerical modelling
Conclusions
Experimental loading rate = 0.2 kN/s

## Slide 20
The numerical model could accurately predict the cracking pattern as well as the sequence of cracking.
Load controlled analysis along with arc length can effectively capture the pre-peak as well as the post-peak zone
By incorporating the tensile constitutive law corresponding to the slower loading rate, we could get good match with the experimental result.
Conclusions
Background
Methodology
Numerical modelling
Conclusions

## Slide 21
THANK YOU