## Slide 1
Numerical Simulation of Splitting and Spalling Fracture in Steel Fibre Reinforced Structural Elements
Dr. Keerthana Kirupakaran, Assistant Professor
Mr. Manas Bhadury, M.S. student
Mr. Filippo Medeghini, PhD student
Dr. Peter Mark, Full Professor
Dr. Giuseppe Tiberti, Associate Professor
Dr. Ivan Trabucchi, Post-doctorate
Dr. Giovanni Plizzari, Full Professor
IIT
MADRAS
BEFIB 2024 XI International Symposium on Fiber Reinforced Concrete September 15-18, 2024

## Slide 2
Background
https://www.reddit.com/r/MachinePorn/comments/125ilo9/tunnel_boring_machine_tbm/
Splitting stresses
Spalling stresses
Lin et al. 2015
Xu et al. 2023
Splitting and spalling cracks
https://www.surechemical.com/aboutus/RP20230823-Fiber-Reinforced-Concrete.html
Steel Fibre Reinforced Concrete
Better crack width control
Faster production compared to RCC segment
Challenges?
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 3
Challenges & Objective
Unlike conventional RCC, Design of SFRC - Fracture mechanics principles
Steel Fibre Reinforced Concrete
Accurate estimation of splitting and spalling stress
Ouyang et al. 2023
Strut and Tie – Elastic analysis – Does not give an accurate prediction of stress for SFRC
Non-linear finite element simulations
Full-scale testing
Expensive
Time consuming
Large scale testing facility
Not straight forward
Material constitutive law
Convergence issues
Experimentally and Numerically assess the spatially optimized SFRC structural elements
OBJECTIVE
Spatial optimization for steel fibre dosage in SFRC
Mechanical performance of spatially optimized SFRC?
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 4
Specimen details
SFRC = 40
SFRC = 40 + 120
SFRC = 40 + 120
(NPFRC)
150
900
150
Thickness = 150 mm
(NPFRC)
(HPFRC)
NPFRC
Steel macro fibers
Hooked-end, 35 mm long, 0.55 mm in diameter
Tensile strength = 1345 MPa
HPFRC 60+60 kg/m3 - Hybrid
Steel micro +macro fibers
Straight, 13 mm long, 0.2 mm in diameter
Tensile strength = 3050 MPa
Steel macro fibers
Hooked-end, 35 mm long, 0.55 mm in diameter
Tensile strength = 1345 MPa
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 5
Loading details
P
P
P
P
Specimen was loaded until failure
Specimen failed under due to tensile splitting
4 LDTs 25 mm
12 LDTs 10 mm
4 LVDTs 10 mm
Instrumentation
Structural engineering lab at UNIBS
SFRC = 40
(NPFRC)
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 6
Numerical Modelling
Modelling assumptions
  2D model
  Plane stress elements
  Smeared crack approach
Material input parameters
  Compressive strength, tensile strength, modulus of elasticity – from experiments & standards
  Uniaxial tensile constitutive law – from inverse analysis
Mesh size: mesh convergence analysis
Loading and support conditions
Analysis input parameters
Numerical results and validation
Key elements
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 7
Numerical Modelling
Material input parameters
NPFRC – 40
Ec= 35009 MPa (retrieved from fcm based on standard)
fcm = 47.04 MPa (experimental tests, assuming fcm0.83fcm,cube)
fctm = MPa [*]
wu =
HPFRC – 120
Ec = 34735 MPa (retrieved from fcm based on standard)
fcm = 45.83 MPa (experimental tests, assuming fcm0.83fcm,cube)
fctm =
wu =
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 8
Numerical Modelling
Constitutive law- Inverse analysis
Material uniaxial tensile constitutive law
Inverse Analysis
curve
Iterative process
Interface element: L8IF
Comparison
Assume
curve
Notch beam model – discrete crack approach
Notch beam experiment
DiANA 10.6 software
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 9
Numerical Modelling
Constitutive law- Inverse analysis
N
w | 
mm | MPa
0 | 3.453
0.023 | 1.56
0.97 | 1.62
2.48 | 1.02
10.15 | 0
()
w | 
mm | MPa
0 | 3.381
0.01 | 2.83
0.3 | 3.4
2.42 | 1.9
10.15 | 0
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 10
Numerical Modelling
CASE 1: SFRC = 40
Element type: CQ16M
Mesh size: Decided based on elastic analysis
For first 20 mm from top :
For rest 580 mm :
Both X and Y-translation: restrained
Total load =
Total load on 16 elements
=
150
Only Y-translation: restrained
150
Y
X
SFRC rectangular segment
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 11
Numerical Modelling
Analysis
CASE 1: SFRC = 40
Node no. | Description | Calculation
10235 | Spalling displacement | 
7095 | Vertical displacement | 
10039 2318 | Splitting displacement | 
Load factor (LF) | Load factor is input | 
Node no. | Description | Calculation
10235 | Spalling displacement | 
7095 | Vertical displacement | 
10039 2318 | Splitting displacement | 
Load factor (LF) | Load factor is input | 
Nodes corresponding to the location of LVDTs
150
900
150
CASE3: SFRC = 40 + 120
CASE 2: 40 + 120
Similar analysis was performed for case 2 & 3
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 12
Numerical Modelling
Analysis preliminary results
Good correlation with first crack load, initial modulus and horizontal portion after first crack load
Unable to capture the subsequent increase in load – convergence issues
Ongoing research – working on simulating the subsequent increase in load after the horizontal portion
CASE 1: SFRC = 40

## Slide 13
Numerical Modelling
Analysis preliminary results
CASE 1: NPFRC 40
From experiments:
Initial spalling cracks occur at 473 kN
Initial splitting cracks occur at 963 kN
After further increase in load splitting failure occurs
From numerical model
Initial spalling cracks occur at 465 kN
Initial splitting cracks occur at 963 kN
After further increase in load – not captured
-1.7% difference between experimental and numerical value
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 14
Numerical Modelling
Analysis preliminary results
CASE 1: NPFRC 40
From experiments:
Initial spalling cracks occur at 473 kN
Initial splitting cracks occur at 963 kN
After further increase in load splitting failure occurs
From numerical model
Initial spalling cracks occur at 465 kN
Initial splitting cracks occur at 947 kN
After further increase in load – not captured
-1.7% difference between experimental and numerical value
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 15
Summary and future work
Simulation of splitting and spalling stress in SFRC segment – complex non-linear FEA
The numerical model gives good correlation with the initial modulus, first crack load and the horizontal portion after the first crack load of the experimental load-displacement curve
Numerical model has captured the initial spalling crack load and initial splitting crack load observed in the experiment
Efforts are ongoing to simulate the subsequent increase in load after the horizontal portion of the experimental load-displacement curve
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.

## Slide 16
Thank you
Keerthana Kirupakaran
keerthanak@civil.iitm.ac.in

## Slide 17
Numerical Modelling
Analysis input parameters
Analysis
Number of load steps and step size is varied
Analysis 1
Analysis 2
Upto first crack
Load step sizes:
Last converged step is saved
Equilibrium iteration:
  Newton-Raphson
  Force norm and displacement norm (convergence tolerance = 0.01)
Post first crack
Load step sizes:
Equilibrium iteration:
  Secant quasi-Newton
  Force norm and displacement norm (convergence tolerance = 0.01)
CASE 1: SFRC = 40
Notes: the cost of AR-glass textiles is about five to six times that of conventional E-glass textiles due to the incorporation of zirconia and the higher energy requirements during manufacturing.