## Slide 1
Numerical Modeling of Flexural behaviour of Textile Reinforced Concrete
Manas Bhadury (M.S. Student)
Keerthana Kirupakaran, Nerswn Basumatary and Tamali Bhowmik
Department of Civil Engineering
Indian Institute of Technology Madras, Chennai India
11th international conference on fracture mechanics of concrete and concrete structures, 10-14th Sept 2023, IISc Bangalore

## Slide 2
Introduction
Literature review
Research gap
Objectives
Methodology
Finite element model
Parametric analysis
Summary and conclusions
Outline

## Slide 3
Textile reinforced concrete
Fine grained concrete
( Aggregate size<2 mm)
Textile
What is TRC?
Introduction
Scheerer et al.
Why TRC ?
More load carrying capacity
More ductility
Lightweight
Yarn

## Slide 4
Number of specimens=4
Number of textile layers=4
Different mesh type=4
Type of loading rate=4
Time consuming and expensive
Way-out ?
Numerical modeling
No. of Experiments = 4^4=256
For each mechanical behaviour
Introduction: Why numerical modelling?

## Slide 5
Literature – Numerical models
Macro scale models
ACK model
OH model
Matrix
Monolithic reinforcement
Matrix
One interface
Matrix
Sleeve filament
Core filament
Sleeve filament
Matrix
Two interface
Von et al.

## Slide 6
Bond in TRC
Banholzer et al.
Literature – Bond

## Slide 7
Analytical bond models
Perfect interface model
No de-bonding
Not suitable
Fracture mechanical model
Cohesive interface model
Literature – Bond
Banholzer et al.

## Slide 8
4-Point bending test setup
Literature – Numerical models
P
P/2
400
185
185
P/2
P
P/2
P/2
400
270
270
Case Study 1
Case Study 2
Textile layer
Portal et al.(2013,2017)

## Slide 9
Literature – Textile modelling(ACK approach)
Rectangular contact perimeter
Warp spacing
Welft
Warp
Contact between yarns
Penetration of concrete matrix
Multi-yarn
Monolithic bar
Portal et al.
Case study-1
Case study-2

## Slide 10
σ
τ
E
Linear elastic constitutive law with no limiting strength
Useful to predict bond failure
Possibility of textile rupture
Literature – Textile modelling(ACK approach)
σ
τ
E
Bi-linear stress-strain curve
Plateau
Portal et al.
Case study-1
Case study-2

## Slide 11
Research gap
Most of the studies have been incorporated to simulate flexural behaviour of the carbon textile reinforced concrete. Flexural behaviour needs to be simulated for glass fiber TRC to incorporate it’s structural applications.
Influence of number of textile layers on flexural performance of TRC has not been considered in most of the studies.

## Slide 12
Objectives
To simulate the flexural behaviour of textile reinforced concrete by incorporating a macro scale model using ACK approach.
To study the effect of textile layers on flexural performance through numerical modelling.

## Slide 13
Priyanga et al.
Defining 2D/3D Model
Results
Post-processing
Mesh
Pre-processing
Material properties
Create geometry
Assign section
Assemble
Interaction
Loading and boundary condition
Check error
Redesign
Methodology
Analysis

## Slide 14
Finite element model
Model geometry in DIANA FEA
Experimental setup: Three point bend test
Nerswn Basumatary

## Slide 15
Finite element model
4 Textile layers
Model geometry in DIANA FEA

## Slide 16
Finite element model
Support and load modelling
Load plate and support plate-
To prevent stress concentration

## Slide 17
Idealization of textile modelling
Schematic of multi-yarn layer
Schematic of monolithic bar
Finite element model-ACK approach
S
Cf
Af
A
C
dx
dx
t
t
Multi-yarn layer
dx
4 no. of monolithic bar
dx

## Slide 18
Concrete
Total strain rotating crack model
Tensile
Compressive
Hordijk constitutive law
Thorenfeldt constitutive law
;= size of element.
Hordijk curve
Thorenfeldt curve
Finite Element Model-model parameters

## Slide 19
Finite Element Model:model parameters
Zone with reduced tensile strength(by 15%)

## Slide 20
σ
τ
E
Linear elastic constitutive law with no limiting strength
Textile
Reinforcement bar
Bond-slip interface
Relative slip(mm)
Bond stress(N/mm2)
Finite Element Model-model parameters
0
0
0.5
10
1
1.5
20

## Slide 21
Finite Element Model-loading parameters
Deformation controlled
Total deformation of 5 mm is applied in 500 load steps.

## Slide 22
Type of elements
Component | No. of elements
Panel | 2240 no. of Q8MEM elements
Load plate | 20 no. of Q8MEM elements
Support plate | 16 no. of Q8MEM elements
Interface between load plate and panel | 20 no. of L8IF elements
Textile reinforcement | 640 no. of bar elements
Q8MEM
L8IF
Finite element model

## Slide 23
Finite Element Model-Analysis
Analysis
Non-linear analysis
Secant( Quasi-newton) method
Convergence norm
Energy=0.001
Displacement=0.01
Force=0.01

## Slide 24
Finite element model
Model result and validation
Results | Experimental | Numerical | Difference(%)
1st Crack Load(N) | 2.273 | 2.076 | 8.65
Deflection at 1st Crack(mm) | 0.20 | 0.28 | 39.30
Load at 0.8 mm deflection(N) | 2.321 | 2.213 | 4.66
0.8
Load (kN)
Mid Span deflection (mm)
0
0.2
0.4
0.6
0
1
0.5
2.5
1.5
2
O
A
B
C
OA-Zone 1
OB-Zone 2
OC-Zone 3
Load (kN)
Mid Span deflection (mm)
0
0.6
0.8
0.4
0.2
2.5
2
1.5
1
0.5
0

## Slide 25
Parametric analysis
Load (kN)
Mid span deflection (mm)
0
1
2
3
0
1
2
3
Parametric analysis: Changing the number of layers of textile

## Slide 26
Parametric analysis
Parametric analysis: Changing the number of layers of textile
Zone 1-OA
Zone 3-AB
k1=540.25 N/mm
k2=1047.33 N/mm
k3=1401.745 N/mm
k4=1630.87 N/mm
Load (kN)
Mid span deflection (mm)
0
1
2
3
0
1
2
3
Load (kN)
Mid span deflection (mm)
Mid span deflection (mm)
Load (kN)
0.5
0.6
0.7
0.8
0.5
1
1.5
2
2.5
0.02
0.04
0.06
0.08
0.1
1
2
3

## Slide 27
Summary and conclusions
Flexural behaviour of textile reinforced concrete has been simulated using macro-scale finite element model based on monolithic bar approach.
The finite element model predicts load-deflection behaviour upto 0.8 mm deflection.
Based on the parametric analysis, it can be concluded that the slope of the strain hardening zone decreases as the number of layers are decreased.

## Slide 28
THANK YOU

## Slide 29
Questions?